## Slide 1: ChE 378 - Materials Science Test 3 Review
Kristie Moffat

## Slide 2: Agenda
ST2 – surface tension, interfacial phenomenon
Ceramics
Cements
Glasses
Metal processing
Heat treatment of metals
Phase change kinetics
Review key topics from last exam
Review of Quiz 10

## Slide 3: Interfacial Phenomena
Definitions
  Surface Free Energy vs. surface tension
  Work of Adhesion
  Spreading
  Adhesion vs Cohesion
  Capillary Action

## Slide 4: Estimating Surface Energy of a Plane - Example
Estimate the surface energy of the (111) plane of gold
  Heat of vaporization = 334.4 kJ/mol
  Atomic radius = 0.144 nm
  Gold has FCC structure
  Atomic mass is 197 g/mol
Notes: Lecture 24 notes also

## Slide 5: Estimating Surface Energy of a Plane – Example, cont.

## Slide 6: Estimating Surface Energy of a Plane – Example, cont.

## Slide 7: More Interfacial Phenomena
Know typical surface energies for metals, amorphous solids, water, ethanol, etc.
LaPlace Equation
  ΔP = 2γ / r
Capillary Rise (Incomplete Wetting)
  h = 2γcosθ / ρgr
Young’s Equation
  Fs = Fsl + Flcosθ
  γsl = γs – γlcosθ
Notes: ST2

## Slide 8: Colloidal Systems
Dispersed Phase/Continuous Phase | Name | Examples
Solid/Liquid | Suspension, gel, paste | Plaster, jello, skim milk
Solid/Gas | Smoke | Smoke, fluidized bed, cirrus clouds
Liquid/Liquid | Emulsion | Latex paint, salad dressing
Liquid/Gas | Fog | Steam, fog, cumulus clouds
Gas/Liquid | Foam | Shaving cream, chocolate mousse
Gas/Solid | Solid Foam | Pumice, styrofoam, bread
Know how to do colloid formation calculations
Colloid stability  ΔG<0 for stable system

## Slide 9: Ceramics (13.6-8, 13.10-11, 14.8-10)
Clay Products
  Structure clay products: bricks, tiles, sewer pipes – structural integrity is important
  Whiteware: porcelain, pottery, tableware, china, plumbing fixtures
Refractories
  Withstand high temperatures without melting or decomposing
  Non-reactive in severe environments
  Fireclay, silica, basic, special refractories

## Slide 10: More Ceramics
Abrasives
  Silicon carbide
  Tungsten carbide
  Aluminum oxide
  Silica sand
Know the specialty ceramics
  Piezoelectrics
  Ceramic Ball Bearings
  Optical Fibers

## Slide 11: Ceramic Processing
Hydroplasticity – when water is added to clay it becomes very plastic
Flux – forms a low melting temperature glass when the clay is fired (feldspar is common)
Finely ground quartz is also added to flux

## Slide 12: Ceramic Processing Techniques
Hydroplastic Forming (extrusion)
Slip Casting (porous mold)
Drying
Firing
Vitrification – gradual formation of liquid glass that fills in the pore volume
  Degree of vitrification controls strength, density, durability of the ceramic

## Slide 13: Ceramic Processing Techniques, cont.
Powder Pressing
  Sintering
Tape Casting
  Substrates for integrated circuits and multilayered capacitors

## Slide 14: Cements
Hydraulic Cement (Portland Cement)
  Hardness reaction occurs with water
  Used as a binder in concrete
Lime
  Non-hydraulic – other compounds than water involved in hardening reaction

## Slide 15: Glass Processing
Know glass transition temperature
Viscosity-Temperature characteristics:
  Melting point
  Working point
  Softening point
  Annealing point
  Strain point

## Slide 16: Soda-Lime Glass
Silica-soda-lime, Na2O and CaO added to quartz
Methods of glass fabrication:
  Pressing
  Blowing
  Drawing
  Sheet forming
  Fiber forming

## Slide 17: Glass Heat Treatment
Annealing
  Glass heated to the annealing point and then slowly cooled to remove internal stresses
Tempering
  Surface in compression and interior in tension
  Discourages the propagation of surface cracks

## Slide 18: Metal Types
Know types of Ferrous Alloys, their compositions and any numbers/names:
  Steels – low carbon, medium carbon, high carbon, stainless
  Cast Irons – gray, ductile (nodular), white, malleable, compacted graphite
Other alloys
  Brass, bronze, aluminum alloys, magnesium alloys, titanium alloys
  Refractory metals, superalloys, noble metals
Notes: 13.1-13.3

## Slide 19: Metal Processing
Cold working v. hot working
Forging, rolling, extruding, drawing
Casting
  Sand, die, investment, lost-foam, continuous
Powder Metallurgy
Welding

## Slide 20: Metal Processing, cont.
Annealing
  Normalizing – refines grains, heat to 55C above upper critical temperature
  Full Annealing – 50C above eutectoid isotherm
  Spheroidizing – Heating to about 700C for long time (15-25 hrs)
Precipitation Hardening

## Slide 21: Phase Change Kinetics
Avrami Equation
  [1 – y = exp(-ktn)]
Notes: Lecture 25 Example – slides 29-32

## Slide 26: Key Topics from Last Exam
Phase Diagrams
Planes and Directions in Crystal Structures
Stress/Strain Curves
Invariant Points
Hume Rothery Rules!

## Slide 28: Common Alloys
Steel (Fe & 0.008 to 2.14 wt% C)
Cast Iron (Fe, Si & 2.14 to 6.7 wt%C)
Stainless Steel (Fe, C, & >11 wt% Cr)
Brass (Cu, Zn)
Bronze (Cu, Sn)
Nitinol (Ni, Ti)
Know properties too!

## Slide 29: Phase Equilibria
Remember Hume-Rothery rules!
Solid solutions – single phase
Invariant Points
  Eutectic – liquid to two solids
  Eutectoid – one solid to two solids
  Peritectic – liquid and solid to another solid
Equilibrium vs. non-equilibrium cooling
Cooling curves
Notes: Lecture 20 notes may be very useful here
Cooling curve – pg 38 of Lecture 20

## Slide 30: Quiz 10 Review
Q: Name two beneficial characteristics of glass.
A: Inexpensive, transparent, ease of manufacture
Q: Name two material properties that ceramic abrasives must have.
A: Toughness, hardness, wear resistance, refractoriness (high temperature resistance)
Q: True or False?
__Hydraulic cement hardens by a chemical process involving water
__Concrete is the same as cement
__Vitrification is the formation of glass during firing of ceramics
__The viscosity of glass increases with temperature
__When making glass, it is common to anneal the finished product to relieve internal stresses
A: T, F, T, F, T

## Slide 31: Quiz 10 Review, Cont.
Q: Describe the raw materials and process steps for soda-lime glass bottle manufacturing.
A: Raw Materials – SiO2 (silica sand), CaO (lime), Na2O (soda)
Process – Mix raw materials, heat, form a “gob”, blow with air into parison mold, anneal
Q: Which of the following are the two primary constituents of clays?
(a) Alumina (Al2O3) and limestone (CaCO3)
(b) Limestone (CaCO3) and cupric oxide (CuO)
(c) Silica (SiO2) and limestone (CaCO3)
(d) Alumina (Al2O3) and Silica (SiO2)
A: (d)

## Slide 32: Quiz 10 Review, Cont.
Q: Match the following metals and metal alloys to their common applications:
Plain Carbon Steel, Brass, Grey Cast Iron, Platinum, Stainless Steel, Titanium Alloy, Magnesium, Aluminum, Tool Steel, Tungsten
High temperature furnace elements in oxidizing atmospheres
Drill bit
Jet engine turbo fan blades, medical implants
Cryogenic (very low temperature) container
Pyrotechnic material (flares, sparklers, fireworks)
Condensing heat exchanger for steam
Block of an internal combustion engine
Wire filaments for light bulbs
Door knobs and common decorative fixtures
Rebar for use in reinforced concrete
(1) Platinum
(2) Tool Steel
(3) Titanium Alloy
(4) Aluminum
(5) Magnesium
(6) Stainless Steel
(7) Grey Cast Iron
(8) Tungsten
(9) Brass
(10) Plain Carbon Steel

## Slide 33: Quiz 10 Review, Cont.
Q: Match the following polymers to their common applications:
Acrylics, Flourocarbons, Nylons, Silicone Rubber, Epoxies, Polycarbonates, Phenolics, Polystyrenes, Vinyls, PET
Automobile engine gaskets, blood tubing, medical implants
Plexiglas, fake fingernails, hard contact lenses
Bearings, gears, cams, bushings, toothbrush bristles
Adhesives, electrical moldings, sinks
Non-stick frying pan, plumber’s tape, vascular graft
Beverage containers, Mylar balloons, clothing fibers
Wall tile, petri dishes, toys, lighting panels, cups for hot drinks
Pipe, garden hoses, phonograph records
Billiard balls, telephones, motor housings, electrical fixtures
Safety helmets, compact discs, bullet proof “glass”
(1) Silicone Rubber
(2) Acrylics
(3) Nylons
(4) Epoxies
(5) Fluorocarbons
(6) PET
(7) Polystyrenes
(8) Vinyls
(9) Phenolics
(10) Polycarbonates

## Slide 34: Quiz 10 Review, Cont.
Q: In production of polymer textile fibers (e.g. for clothing), why is it necessary to use polymers of high molecular weight?
A: To provide sufficient strength (e.g. not to break during the fiber drawing process)
Q: Amorphous thermoplastics are formed above their:
(a) Glass transition temperatures
(b) Softening points
(c) Melting temperatures
(d) none of the above
A: (a)
Q: Describe mechanical and chemical bonding mechanisms by which polymeric adhesives act.
A: Mechanical bonding: the adhesive penetrates into the surface pores and crevices
Chemical bonding: the adhesive establishes covalent or Van der Waals forces with the adherend.